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AIMOL GREASELINE LITHIUM COMPLEX EP
High performance grease for high temperatures
Description

AIMOL GREASELINE LITHIUM COMPLEX EP is a complex grease with EP additives for medium speed operated bearings and plain bearings. They are provided with resistance to water and excellent resistance to high temperatures and loads.
Applications

AIMOL GREASELINE LITHIUM COMPLEX EP can be used as long life grease in roller bearings, water pumps, electric motors, couplings, cardan joints and in general wherever high efficiency greases are needed with severe requirements.
Benefits

· High dropping point 

· Good resistance to heavy loads

· Outstanding anti wear capacity

· Insoluble in water 

· Good resistance to mechanic work

· Good protection against corrosion
· Good antioxidant capacity 
· Long life
Typical performance data
	
	Test method
	EP 00
	EP 1
	EP 2

	Thickener, soap type
	
	Lithium complex

	Base oil nature
	
	Mineral

	Colour
	
	Amber
	Brown
	Blue

	Base oil viscosity @ 40 °C, cSt
	
	220
	220
	220

	NLGI consistency class
	DIN 51818
	00
	1
	2/3

	Penetration 60W, x 0,1 mm
	ASTM D217
	400-430
	265-295
	245-265

	Dropping point, ºC
	ASTM D566
	>200
	>240
	>245

	EMCOR corrosion test 
	DIN 51802
	1
	1
	1

	Copper corrosion, 4h/100 ºC
	ASTM D130
	1b
	1b
	1b

	4-ball wear test

· Welding load, kg

· Scar diameter 1h/40kg, mm
	IP-239
	450

0,55
	450

0,55
	450

0,55

	Evaporation loss @ 22h/100 ºC, %
	ASTM D972
	0,5
	0,5
	0,5

	Water resistance, 90 ºC
	DIN 51807
	1
	1
	1

	Service temperature, ºC
	
	-15 – 130
	-30 – 150
	-30 – 150


TECHNICAL DATA INFO LINE

Should you require additional information or advice on AIMOL products, please contact us as per the details below.  

HEALTH AND SAFETY  

AIMOL GREASELINE LITHIUM COMPLEX EP has no adverse health effects provided it is used as directed.  

DISCLAIMER 

Typical figures as indicated may vary per production cycle and can change at manufacturers’ option. Specifications, however, are guaranteed. Because of continuous product research and development, the information within this data sheet is subject to change without any notification. Although every effort is made to ensure accurate information, A.I.M. bv accepts no liability for any loss or damage suffered caused by the incorrectness and/or incompleteness of this text, and as a result of using this product for any application other than explicitly stated in this data sheet. [image: image1.jpg]
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